## Slide 1: Towards Multi-Permeability Cores Through Composition-Controlled Pellet Extrusion
Brainstorming

## Slide 2: Agenda
Who am I?
Introduction to additive manufacturing (AM)
My previous work
Constant flux inductor (CFI)
Multi-permeability magnetic cores
Current field of 3D printing magnetics
Outlined research direction
Research questions
Requirements and methodology
Potential collaboration

## Slide 3: Who am I?
Artis Fils
Experience:
BSc in Mechatronics from University of Southern Denmark (SDU)
MSc in Mechatronics from University of Southern Denmark (SDU)
Additive Manufacturing student worker for 4.5 years
Interests:
Additive manufacturing
3D printed electronics
Hybrid manufacturing
Currently:
Research assistant focusing on 3D printing magnetics

## Slide 4: What is additive manufacturing?

## Slide 5: What is additive manufacturing?

## Slide 6: Why additive manufacturing?
Advantages
Fast design iterations
Cheaper failures
Complex geometries
Lighter stronger parts
On demand manufacturing
Waste reduction
Multi material capabilities
Disadvantages
Slow
Resolution & surface finish
Size constraints
Hardware reliability
Material limitations
Expensive at scale

## Slide 7: 3D printing vs additive manufacturing
Model
Slice
Print

## Slide 8: Most common methods of additive manufacturing

## Slide 9: What is Fused Deposition Modeling (FDM)?

## Slide 10: What is Fused Deposition Modeling (FDM)?

## Slide 11: BSc Thesis and Publication
“From Composite Filaments to Low-loss Circuits: A Novel Hybrid Manufacturing Approach to 3D-Printed Electronics”
FDM
Electroplating

## Slide 12: BSc Thesis and Publication
“From Composite Filaments to Low-loss Circuits: A Novel Hybrid Manufacturing Approach to 3D-Printed Electronics”
Cup-based electroplating

## Slide 13: BSc Thesis and Publication
“From Composite Filaments to Low-loss Circuits: A Novel Hybrid Manufacturing Approach to 3D-Printed Electronics”
Cup-based electroplating
Physical setup

## Slide 14: BSc Thesis and Publication
“From Composite Filaments to Low-loss Circuits: A Novel Hybrid Manufacturing Approach to 3D-Printed Electronics”
Cup-based electroplating
Physical setup
Resulting speaker

## Slide 15: MSc Thesis
“Recyclable 3D Printing of Aqueous PNIPAM for Sustainable Electroforming”

## Slide 16: MSc Thesis
“Recyclable 3D Printing of Aqueous PNIPAM for Sustainable Electroforming”
PNIPAM solidification cycle

## Slide 17: MSc Thesis
“Recyclable 3D Printing of Aqueous PNIPAM for Sustainable Electroforming”
PNIPAM solidification cycle
Electroforming

## Slide 18: MSc Thesis
“Recyclable 3D Printing of Aqueous PNIPAM for Sustainable Electroforming”
Developed 3D printer

## Slide 19: MSc Thesis
“Recyclable 3D Printing of Aqueous PNIPAM for Sustainable Electroforming”
Developed 3D printer
PNIPAM/CNT specimen

## Slide 20: MSc Thesis
“Recyclable 3D Printing of Aqueous PNIPAM for Sustainable Electroforming”
Developed 3D printer
PNIPAM/CNT specimen
PNIPAM/CNT electroform

## Slide 21: Constant-flux inductor (CFI)
A constant-flux inductor is an magnetic component designed to distribute magnetic flux uniformly across its core.

## Slide 22: Constant-flux inductor (CFI)
A constant-flux inductor is an magnetic component designed to distribute magnetic flux uniformly across its core.
Benefits:
Prevents localized saturation
Distributes the temperature
Reduces the footprint

## Slide 23: Constant-flux inductor (CFI)
A constant-flux inductor is an magnetic component designed to distribute magnetic flux uniformly across its core.
Benefits:
Prevents localized saturation
Distributes the temperature
Reduces the footprint
Tradeoff:
Manufacturing complexity
Cost
Physical tuning

## Slide 24: Methods of designing a CFI
Specialized geometry
Multi-permeability

## Slide 25: Methods of designing a CFI
Specialized geometry
Multi-permeability

## Slide 26: Methods of designing a CFI
Specialized geometry
Multi-permeability

## Slide 27: Methods of designing a CFI
Geometry and permeability are not mutually exclusive design variables, and optimizing both may offer further benefits.
Custom and complex -> perfectly suited for AM.
Specialized geometry
Multi-permeability

## Slide 28: Methods of manufacturing a multi-permeability core
Multi-step pressing
Complex tooling
Limited design freedom

## Slide 29: Methods of manufacturing a multi-permeability core
Multi-step pressing
Temperature gradient sintering
Complex tooling
Limited design freedom
Complex sintering
Limited design freedom

## Slide 30: Methods of manufacturing a multi-permeability core
Multi-step pressing
Temperature gradient sintering
Multi-material AM
Complex tooling
Limited design freedom
Complex sintering
Limited design freedom
Requires sintering

## Slide 31: Current field of 3D printing magnetics
3D printing magnetics
Vat polymerization
Powder bed fusion
Binder jetting
Material extrusion
Fused deposition modeling
Direct ink writing
Fused granulate fabrication

## Slide 32: Current field of 3D printing magnetics
3D printing magnetics
Vat polymerization
Powder bed fusion
Binder jetting
Material extrusion
Fused deposition modeling
Direct ink writing
Fused granulate fabrication
Inability to perform multi-material printing in the same layer

## Slide 33: FDM vs FGF vs DIW
Fused Deposition Modeling (FDM)
Fused Granulate Fabrication (FGF)
Direct Ink Writing (DIW)

## Slide 34: Current field of 3D printing magnetics
3D printing magnetics
Vat polymerization
Powder bed fusion
Binder jetting
Material extrusion
Fused deposition modeling
Direct ink writing
Fused granulate fabrication
μr = 42
μr = 35 - 500
μr = 1.4 - 4
Inability to perform multi-material printing in the same layer

## Slide 35: Current field of 3D printing magnetics
3D printing magnetics
Vat polymerization
Powder bed fusion
Binder jetting
Material extrusion
Fused deposition modeling
Direct ink writing
Fused granulate fabrication
μr = 42
μr = 35 - 500
μr = 1.4 - 4
Inability to perform multi-material printing in the same layer
Low permeability

## Slide 36: Current field of 3D printing magnetics
3D printing magnetics
Vat polymerization
Powder bed fusion
Binder jetting
Material extrusion
Fused deposition modeling
Direct ink writing
Fused granulate fabrication
μr = 42
μr = 35 - 500
μr = 1.4 - 4
Inability to perform multi-material printing in the same layer
Low permeability
Requires sintering

## Slide 37: Current field of 3D printing magnetics
3D printing magnetics
Vat polymerization
Powder bed fusion
Binder jetting
Material extrusion
Fused deposition modeling
Direct ink writing
Fused granulate fabrication
μr = 42
μr = 35 - 500
μr = 1.4 - 4
Inability to perform multi-material printing in the same layer
Low permeability
Requires sintering
Selected

## Slide 38: Research direction
Fused Granulate Fabrication (FGF)
Multi-permeability cores

## Slide 39: Multi-permeability via different materials
PA12 with x wt% FeSiAl (μrx)
PA12 with y wt% FeSiAl (μry)
PA12 with z wt% FeSiAl (μrz)

## Slide 40: Multi-permeability via different materials
PA12 with x wt% FeSiAl (μrx)
PA12 with y wt% FeSiAl (μry)
PA12 with z wt% FeSiAl (μrz)

## Slide 41: Multi-permeability via mixing different ratios
PA12 with 86 wt% FeSiAl (μr_100:0)
PA12

## Slide 42: Multi-permeability via mixing different ratios
μr_25:75
PA12 with 86 wt% FeSiAl (μr_100:0)
PA12

## Slide 43: Multi-permeability via mixing different ratios
μr_25:75
μr_75:25
PA12 with 86 wt% FeSiAl (μr_100:0)
PA12

## Slide 44: Research questions
Can varying the blend ratio of magnetic-filled and unfilled polymer pellets produce reproducible changes in the permeability of a soft-magnetic composite manufactured using a commercial pellet extruder?
μr_25:75_1 = μr_25:75_2 ?
μr_75:25_1 = μr_75:25_2 ?

## Slide 45: Requirement and methodology – Nr. 1
Requirement
Establish a repeatable pellet-extrusion process for producing test specimens from the selected magnetic-filled and unfilled polymer pellets.
Methodology
Conduct a targeted review of commercially available pellet extruders and compatible polymer feedstocks.
Create an evaluation matrix, setting out project criterion with their specific weight. Select the highest rated path of solutions. Develop and assemble the selected manufacturing process.
Investigate appropriate printing parameters.

## Slide 46: Requirement and methodology – Nr. 2
Requirement
Quantify bulk filler-content variation and local FeSiAl distribution in a representative 50:50 pellet blend across selected extrusion positions and repeat runs.
Methodology
Manufacture a homogeneity specimen at 50:50 blend ratio.
Use Thermogravimetric Analysis (TGA) to estimate bulk filler content, calibrated to the known filler content.
Scanning Electron Microscopy paired with Energy-Dispersive X-ray Spectroscopy (SEM–EDS) mapping of cross-sections to quantify local FeSiAl distribution.
Samples from independent extrusion runs and different specimen locations will be analysed to assess compositional variation, mixing homogeneity and run-to-run reproducibility.

## Slide 47: Requirement and methodology – Nr. 3
Requirement
Determine the effective permeability and between-specimen variability for five magnetic filled-to-unfilled pellet mass ratios (0:100, 25:75, 50:50, 75:25 and 100:0), using three independently printed specimens per ratio.
Methodology
Choose and design a fixed rectangular toroid specimen geometry.
Using the developed manufacturing process, fabricate three specimen at each specific (0:100, 25:75, 50:50, 75:25, 100:0) magnetic-filled-to-unfilled pellet mass ratios.
Ensure that the printing parameters are constant.
Wind the same number of turns of isolated copper wire around each specimen, ensuring consistent winding arrangement.
Measure the inductance and it’s between-specimen variability using an impedance analyzer across a specific frequency range.
Calculate the effective permeability.

## Slide 48: Research questions
Can discrete permeability regions be fabricated by sequentially printing pre-blended pellet batches, using controlled purging to achieve distinct and reproducible material compositions?

## Slide 49: Requirement and methodology – Nr. 4
Requirement
Establish a repeatable pause–purge–resume procedure that limits residual material from the previous pellet batch when switching blend ratios.
Methodology
To determine the required purge amount, a print will be paused after reaching steady state extrusion with a 0:100 blend, and the remaining pellets will be removed from the hopper before loading the 100:0 blend.
The extruder will then be purged into separately collected samples at defined cumulative extruded masses.
TGA will be used to estimate the composition of each sample, using known blend ratios to establish a calibration.
The composition will be plotted against the cumulative purge mass to determine how much material must be purged before the new blend reaches a stable composition.
The procedure will be repeated to additionally for the transition from 100:0 to 0:100 ratio.

## Slide 50: Requirement and methodology – Nr. 5
Requirement
Evaluate the feasibility of fabricating a core with three distinct permeability regions by sequentially printing pre-blended pellet batches.
Methodology
Design a toroidal core with a rectangular cross-section and three regions (100:0, 75:25 and 50:50) arranged to accommodate sequential material changes. Assign each region a blend ratio based on the experimentally characterized permeability values.
Manufacture the core using the established pause-purge-resume procedure.
Visually assess whether the intended regions have distinct compositions.

## Slide 51: Requirement and methodology – Nr. 6
Requirement
Characterise the three-region core's inductance and, where resources permit, saturation behaviour and core losses, and compare its performance with a uniform-permeability reference core of identical geometry.
Methodology
Wind the same amount of turns of isolated copper wire around the manufactured core.
Measure the inductance of the multi-permeability specimen and uniform permeability specimen with a impedance analyser across a specific frequency range.
Remove the winding.
Wind an excitation coil and a separate sensing coil around the core.
Drive the excitation coil with a controlled AC source.
Measure the excitation current and sensing coil voltage.
Calculate the magnetic field strength and flux density.
To measure the core losses, adjust the source so the core reaches the peak flux density.
Record the B-H loop.
Calculate the energy loss from its enclosed area. Repeat the procedures for uniform permeability specimen.
Compare the resuls.

## Slide 52: Potential collaboration areas
Current scope:
Help with magnetic core geometry and measuring effective permeability.
Help setting up Characterizing saturation behavior and core losses.
Simulation of multi-permeability cores.
Design of multi-permeability cores.
Distant future:
Design of CFI with tailored geometry and multi-permeability.
Automating multi-material capabilities for FGF.
Research immersion or colleague collaboration?

## Slide 53: Summary
Constant flux inductors (CFI) are beneficial with a complexity tradeoff.
Multi-permeability cores are an approach to produce CFI.
Additive manufacturing (AM) provides multi-material and complex geometry capabilities.
Established AM method of manufacturing CFIs require complex post-processing.
Fused Granulate Fabrication (FGF) does not require post-processing although produces lower permeability magnetic cores.
Whether FGF can be used to manufacture multi-permeability cores is unanswered.
Requirements and methodology attempt to address the research questions.
There are potential collaboration opportunities.